New materials based on doped single-wall carbon nanotubes or graphene

E.D. Obraztsova1*, A.A.Tonkikh1, V.I. Tsebro2, D.V. Rybkovskiy1, M.G. Rybin1, E.A. Obraztsova1,3, E.I. Kauppinen4, A.S. Orekhov1, A.L. Chuvilin5

1 A.M. Prokhorov General Physics Institute, RAS, 38 Vavilov street, 119991 Moscow, Russia

2 P.N. Lebedev Physical Institute, RAS, Leninskiy prosp., 53, 119991 Moscow, Russia

3 M.M. Shemyakin and Yu.A. Ovchinnikov Institute of Bioorganic Chemistry, RAS, Moscow, Russia

4 Dep. of Appl. Physics, Aalto University, FI-00076 Espoo, Finland

5 CIC NanoGUNE Consolider, San Sebastian 20018, Spain

elobr@mail.ru

Gas phase filling of inner space of single-wall carbon nanotubes integrated into thin films by donor or acceptor molecules or covering graphene by a thin film of such molecules allow to form a new prospective material for transparent conductive electrodes with characteristics comparable with those of indium-tin oxide (ITO).

From HRTEM images formation of one-dimensional crystals inside nanotubes has been revealed. The optical spectroscopy has shown a Fermi level shift into a valence band and a complete metallization of the nanotubes. The effect was more pronounced for the initially pure metallic nanotubes.

Fig.1. One-dimensional crystals formed inside SWNTs from donor or acceptor molecules.

To confirm metallization we have measured the electrical resistance of filled SWNT films of different transparency and registered a big drop of electrical resistance (of one order of magnitude) after filling. The best values were 50 Ohm/square at 90% transparency.

The temperature dependence of resistance (R(T)) demonstrated two contributions – from the inter-tube interactions and from the filled nanotubes by themselves. For the stronger acceptor (CuCl instead of iodine) the minimum value of R(T) shifted toward low temperatures.

This approach opens a new way to form the electrodes for solar cells and optoelectronic devices.

The work was supported by RSF project 15-12-30041. E.A.O. thanks project RFBR-15-32-70014_mol_a_mos for support.